FINISHED PRODUCT SPECIFICATION SHEET

HairTite XL Beard Snood

Material					Polypropylene 56 decitex

(ISO 9001 accredited supplier)

Elastic					Nylon covered rubber.  Min. 3x stretch

Width (qty of yarn strands)		103

Size (stretched)				43cm

Fabric Structure				HairTite HiCare

Weight					3 grams

Dye Fastness				4/5 grey scale C06A2S

Metal Detectable				Same cost option for due diligence

Quantities					Inner			Outer Case

36 pcs packed loose in polybag

Features and Benefits: HairTite Beard Snood

- Independently tested for hair containment by the University of Bolton UK

  - 2 X better hair containment than a traditional 5mm mesh beard net

- Only hair containment product to be certified and approved by HACCP International as suitable for use within food processing and food service environments

- Tested for harmful substances in accordance with Oeko-Tex Standard 100

- Mesh used is Flame retardant to BSEN ISO 1021 – 1:2006

- Contains Prolen: moisture wicking properties for optimum wearer comfort and temperature regulation

- Available metal free and metal detectable

For optimum hair containment read the White Paper Target Zero Hair Complaints: www.aburnet.co.uk/target-zero-hair-complaints/